## Slide 1: Structural Performance of Texas U-Beams at Prestress Transfer and Under Shear-Critical Loads
Catherine Hovell
July 26, 2011
…the culmination of four years of hard work…

## Slide 2: Acknowledgements
Alejandro Avendaño (PhD 2011)
Andy Moore (MSE 2010)
Dave Dunkman (MSE 2009)
Eisuke Nakamura (MSE 2011)
David Langefeld (MSE)
Brian Hanson (MSE)
David Wald (BS 2010)
Stephanie German (BS 2009)

## Slide 3: Flow of Test Program
Can we optimize the end-region of Texas U-Beams?
  ease construction
  maintain structural performance

## Slide 4: Flow of Test Program
Literature Review:
  Previous testing of U-Beams
  Structural performance – at prestress transfer and under shear-critical loads

## Slide 5: Flow of Test Program
at prestress transfer
under shear-critical loads
build U-Beams!

## Slide 6: Flow of Test Program
at prestress transfer
under shear-critical loads
build U-Beams!

## Slide 7: Flow of Test Program

## Slide 8: Presentation Goals
Present the details of this project, and the most valuable conclusions about the behavior of U-Beams:
  at prestress transfer
  under shear-critical loads

## Slide 9: Presentation Outline
Introduce the Texas U-Beam
Discuss:
  prestress transfer
  shear testing
Test program
Expectations
Results
Conclusions

## Slide 10: Introduction to the Texas U-Beam
Designed in the 1990s as an "aesthetically pleasing" alternative for use in highly visible interchanges
  matched popular steel tub girders
  fewer breaklines

## Slide 11: Introduction to the Texas U-Beam
Designed in the 1990s as an "aesthetically pleasing" alternative for use in highly visible interchanges
  matched popular steel tub girders
  fewer breaklines
Meant to replace two AASHTO Type IV girders
[ Ralls, Ybanez, and Panak, PCI, 1993 ]

## Slide 12: Introduction to the Texas U-Beam
96"
5"
4
1
55"
54"

## Slide 13: PRESTRESS TRANSFER

## Slide 14: U-Beams Monitored at Prestress Transfer
Four beams, resulting in eight end-regions
Variables included:
  External skew
  Void skew
  Prestressing force
  Amount of reinforcement
  Beam cross-section
All built at FSEL
Beam 1
Beam 2
Beam 3
Beam 4

## Slide 15: Beam Fabrication
tie reinforcement

## Slide 16: Beam Fabrication
install instrumentation

## Slide 17: Beam Fabrication
stress prestressing strands

## Slide 18: Beam Fabrication
place concrete: fill bottom slab

## Slide 19: Beam Fabrication
place concrete: place void form

## Slide 20: Beam Fabrication
place concrete: fill webs

## Slide 21: Beam Fabrication
place concrete: clean up

## Slide 22: Beam Fabrication
…wait…

## Slide 23: Beam Fabrication
remove void

## Slide 24: Beam Fabrication
release strands, record data

## Slide 25: Reinforcing Bar Instrumentation
strain gauges
strain in gauge, equal to strain in reinforcing bar
“measured stress”
= 29,000 ksi

## Slide 26: Expectations: Behavior at Prestress Transfer
From AASHTO LRFD (2010):
  Steel should be provided transverse to prestressing strands, to resist 4% of the prestressing force without straining bars within h/4 from beam end beyond 20 ksi.
stress expected;
ideally < 20 ksi

## Slide 27: Expectations: Behavior at Prestress Transfer
Critical point:
  Prestress transfer should not significantly stress reinforcing bars counted towards shear capacity
cannot be
used twice
stress expected;
ideally < 20 ksi

## Slide 28: Expectations: Behavior at Prestress Transfer
Previous research summarized in a database compiled by Dunkman (2009 MSE thesis)
  Five references from 1962-2007
  Fifty-three data points (45 I-beams, 8 inverted-Ts)

## Slide 29: Expectations: Behavior at Prestress Transfer
Prestressing Force [kip]
Total Transverse Force within [kip]

## Slide 30: Expectations: Behavior at Prestress Transfer
Prestressing Force [kip]
4%
Total Transverse Force within [kip]
AASHTO design stress

## Slide 31: Expectations: Behavior at Prestress Transfer
Prestressing Force [kip]
4%
Total Transverse Force within [kip]
Now, let’s add U-Beams

## Slide 32: Observations: Behavior at Prestress Transfer
Prestressing Force [kip]
4%
Total Transverse Force within [kip]

## Slide 33: Conclusions: Behavior at Prestress Transfer
AASHTO design assumption that transverse force is equal to 4% of prestressing force:
  is conservative for U-Beams
  is conservative at higher levels of prestressing
Reinforcement in current standard is sufficient to control cracks
Reinforcing bar stresses induced at prestress transfer do not influence vertical shear strength
4%

## Slide 34: Observations: Behavior at Prestress Transfer
Test Region B2N
NORTH
NORTHEAST
NORTHWEST

## Slide 35: Observations: Behavior at Prestress Transfer
Test Region B2N
NORTH
NORTHEAST
NORTHWEST
crack width typically < 0.013 in.

## Slide 36: Conclusions: Behavior at Prestress Transfer
AASHTO design assumption that transverse force is equal to 4% of prestressing force:
  is conservative for U-Beams
  is conservative at higher levels of prestressing
Reinforcement in current standard is sufficient to control cracks
Reinforcing bar stresses induced at prestress transfer do not influence vertical shear strength

## Slide 37: Observations: Behavior at Prestress Transfer
Test Region B2N
NORTH
NORTHEAST
NORTHWEST

## Slide 38: Observations: Behavior at Prestress Transfer
Test Region B2N
NORTH
NORTHEAST
NORTHWEST
Size and color of circles represent magnitude of measured stresses
1 ksi
10 ksi
20 ksi

## Slide 39: Conclusions: Behavior at Prestress Transfer
AASHTO design assumption that transverse force is equal to 4% of prestressing force:
  is conservative for U-Beams
  is conservative at higher levels of prestressing
Reinforcement in current standard is sufficient to control cracks
Reinforcing bar stresses induced at prestress transfer are not significant in shear region

## Slide 40: SHEAR STRENGTH

## Slide 41: U-Beams Tested Under Shear-Critical Loads
Phase I and Phase II Beams
  Phase I: beam details follow existing TxDOT standard drawings
  Phase II: beam details are modified in some way

## Slide 42: Shear Test Setup
Two 2M lb rams
4M lb reaction structure
post-tensioned clamps
bars at 4 in.
bars at 6 in.
= 2.6

## Slide 43: Shear Test Setup
Two 2M lb rams
4M lb reaction structure
post-tensioned clamps
bars at 4 in.
bars at 6 in.
FAILURE ZONE
= 2.6

## Slide 44: Shear Test Setup

## Slide 45: Expectations: Shear Strength
University of Texas Prestressed Concrete Shear Database (2011 Edition) [ UTPCSDB-2011 ]
  99 references from 1954-2010
  shear studies from US, Europe, Japan
  summarized in Eisuke Nakamura’s thesis (May, 2011)

## Slide 46: UTPCSDB-2011
Collection Database | 1688 tests

## Slide 47: UTPCSDB-2011
Collection Database |  | 1688 tests
Filtering Criteria: remove tests irrelevant to the shear behavior of prestressed concrete members | Failure modes other than shear failure (flexural, bond, bearing) | - 417 tests
 | Nonprestressed member | - 156 tests
 | Missing applied load at failure | - 6 tests
 | With initial defects | - 4 tests
 | Subjected to moving loads | - 7 tests

## Slide 48: UTPCSDB-2011
Collection Database |  | 1688 tests
Filtering Criteria: remove tests irrelevant to the shear behavior of prestressed concrete members | Failure modes other than shear failure (flexural, bond, bearing) | - 417 tests
 | Nonprestressed member | - 156 tests
 | Missing applied load at failure | - 6 tests
 | With initial defects | - 4 tests
 | Subjected to moving loads | - 7 tests

## Slide 49: UTPCSDB-2011
Collection Database |  | 1688 tests
Filtering Criteria: remove tests irrelevant to the shear behavior of prestressed concrete members | Failure modes other than shear failure (flexural, bond, bearing) | - 417 tests
 | Nonprestressed member | - 156 tests
 | Missing applied load at failure | - 6 tests
 | With initial defects | - 4 tests
 | Subjected to moving loads | - 7 tests
Filtered Database |  | 1138 tetsts

## Slide 50: UTPCSDB-2011
Collection Database |  | 1688 tests
Filtering Criteria: remove tests irrelevant to the shear behavior of prestressed concrete members | Failure modes other than shear failure (flexural, bond, bearing) | - 417 tests
 | Nonprestressed member | - 156 tests
 | Missing applied load at failure | - 6 tests
 | With initial defects | - 4 tests
 | Subjected to moving loads | - 7 tests
Filtered Database |  | 1138 tetsts
Filtering Criteria: remove tests not deemed useful for the evaluation of the shear design provisions | Concrete strength < 4 ksi | - 162 tests
 | Concrete types other than normal concrete | - 59 tests
 | Member height < 12.0 in. | - 337 tests
 | Shear span-to-depth ratio < 2.0 (concentrated loads) | - 119 tests
 | Insufficient amount of shear reinforcement (per ACI 318-08) (per AASHTO LRFD 2010) | - 644 tests - 631 tests
 | Continuous beams | - 37 tests
 | Segmental specimens | - 18 tests
 | Externally post-tensioned specimens | - 35 tests

## Slide 51: UTPCSDB-2011
Collection Database |  | 1688 tests
Filtering Criteria: remove tests irrelevant to the shear behavior of prestressed concrete members | Failure modes other than shear failure (flexural, bond, bearing) | - 417 tests
 | Nonprestressed member | - 156 tests
 | Missing applied load at failure | - 6 tests
 | With initial defects | - 4 tests
 | Subjected to moving loads | - 7 tests
Filtered Database |  | 1138 tetsts
Filtering Criteria: remove tests not deemed useful for the evaluation of the shear design provisions | Concrete strength < 4 ksi | - 162 tests
 | Concrete types other than normal concrete | - 59 tests
 | Member height < 12.0 in. | - 337 tests
 | Shear span-to-depth ratio < 2.0 (concentrated loads) | - 119 tests
 | Insufficient amount of shear reinforcement (per ACI 318-08) (per AASHTO LRFD 2010) | - 644 tests - 631 tests
 | Continuous beams | - 37 tests
 | Segmental specimens | - 18 tests
 | Externally post-tensioned specimens | - 35 tests

## Slide 52: UTPCSDB-2011
Collection Database |  | 1688 tests
Filtering Criteria: remove tests irrelevant to the shear behavior of prestressed concrete members | Failure modes other than shear failure (flexural, bond, bearing) | - 417 tests
 | Nonprestressed member | - 156 tests
 | Missing applied load at failure | - 6 tests
 | With initial defects | - 4 tests
 | Subjected to moving loads | - 7 tests
Filtered Database |  | 1138 tetsts
Filtering Criteria: remove tests not deemed useful for the evaluation of the shear design provisions | Concrete strength < 4 ksi | - 162 tests
 | Concrete types other than normal concrete | - 59 tests
 | Member height < 12.0 in. | - 337 tests
 | Shear span-to-depth ratio < 2.0 (concentrated loads) | - 119 tests
 | Insufficient amount of shear reinforcement (per ACI 318-08) (per AASHTO LRFD 2010) | - 644 tests - 631 tests
 | Continuous beams | - 37 tests
 | Segmental specimens | - 18 tests
 | Externally post-tensioned specimens | - 35 tests
Evaluation Database – Level I |  | 216 tests

## Slide 53: UTPCSDB-2011
Evaluation Database – Level I |  | 216 tests
Filtering Criteria: remove tests controlled by non-traditional failure modes | Signs of horizontal shear | - 22 tests
 | Signs of anchorage failure / strand slip | - 30 tests

## Slide 54: UTPCSDB-2011
Evaluation Database – Level I |  | 216 tests
Filtering Criteria: remove tests controlled by non-traditional failure modes | Signs of horizontal shear | - 16 tests
 | Signs of anchorage failure / strand slip | - 30 tests

## Slide 55: UTPCSDB-2011
Evaluation Database – Level I |  | 216 tests
Filtering Criteria: remove tests controlled by non-traditional failure modes | Signs of horizontal shear | - 16 tests
 | Signs of anchorage failure / strand slip | - 30 tests
Evaluation Database – Level II |  | 170 tests

## Slide 56: Expectations: Shear Strength
Concrete Strength [ksi]
calculated using AASHTO LRFD General Procedure (2010)
conservative

## Slide 57: Expectations: Shear Strength
Concrete Strength [ksi]
calculated using AASHTO LRFD General Procedure (2010)
conservative

## Slide 58: Beams 1 and 2
Beam 1
Beam 2
B1N
B1S
B2N
Failure could not be reached
B2S

## Slide 59: Shear Performance: B1N
= [0.71]
[0.89]
Shear Force
Distance from Beam End
#4 R-bars (stirrups) spaced at:
  4 in. for 6'-3"
  6 in. for 7'-1"
B1N = 659 kip
= 0.71

## Slide 60: Shear Performance: B1N
Concrete Strength [ksi]
calculated using AASHTO LRFD General Procedure (2010)
conservative
B1N

## Slide 61: Shear Performance: B1S & B2N
Shear Force
Distance from Beam End
= [0.82]
[0.66]
= 0.66
B1S

## Slide 62: Shear Performance: B1S & B2N
= [0.82]
[0.66]
Shear Force
Distance from Beam End
= 0.66
= [0.56]
[0.72]
Shear Force
Distance from Beam End
= 0.56
B1S
B2N

## Slide 63: Intermediate Analysis
These beams are not failing in web-shear
Are we testing the worst-case scenario?
Beam 3
B3N
B3S
46% of strands (36 of 78) debonded at beam end

## Slide 64: Shear Performance: B3N & B3S
Shear Force
Distance from Beam End
Shear Force
Distance from Beam End
= [0.96]
[1.07]
= 0.96
= [1.08]
[0.97]
= 0.97
B3N
B3S

## Slide 65: Comparison of Failure Shears
Failure Shear, [kip]
B1N
B1S
B2N
B3N
B3S
659 k
612 k
610 k
655k
663 k
0.66
0.56
0.96
0.97
0.71

## Slide 66: Shear Performance: B3S
B3S

## Slide 67: SHEAR STRENGTH: Horizontal Shear in Prestressed Beams

## Slide 68: Horizontal Shear in Prestressed Beams
P
reinforcement

## Slide 69: Horizontal Shear in Prestressed Beams
P

## Slide 70: Horizontal Shear in Prestressed Beams
P

## Slide 71: Horizontal Shear in Prestressed Beams
P

## Slide 72: U-Beams Tested Under Shear-Critical Loads
Phase I and Phase II Beams
  Phase I: beam details follow existing TxDOT standard drawings
  Phase II: beam details are modified in some way
    Test regions B4N, B4S, and B5N contained different designs intended to control horizontal shear
    Test regions B6S and B7N tested a single design meant for implementation into the TxDOT standard



## Slide 73: Test Region B4N
#4 R-bars spaced at 3 in. for 5'-0"
4 in. for 5'-0"
6 in. for 3'-4"
modified cross-section
confinement steel
R-bar

## Slide 74: Test Region B4N
Shear Force
Distance from Beam End
horizontal shear with some web crushing
= [0.86]
[1.12]
[0.93]
= 0.86
#4 R-bars spaced at 3 in. for 5'-0"
4 in. for 5'-0"
6 in. for 3'-4"
B4N

## Slide 75: Test Region B4S
#4 R-bars spaced at 3 in. for 5'-0"
4 in. for 5'-0"
6 in. for 3'-4"
3-#5 S-bars spaced at 3 in. for 5'-0"
4 in. for 2'-8"
modified cross-section
confinement steel
supplementary bottom flange-to-web steel (S-bars)
R-bar

## Slide 76: Test Region B4S
Shear Force
Distance from Beam End
#4 R-bars spaced at 3 in. for 5'-0"
4 in. for 5'-0"
6 in. for 3'-4“
3-#5 S-bars spaced at 3 in. for 5'-0"
4 in. for 2'-8"
= 1.37
[1.37]
[1.05]
[1.14]
test halted before failure
B4S
No S-bars

## Slide 77: Test Region B5N
#5 R-bars spaced at 4 in. for 8'-3"
6 in. for 5'-1"
#6 L-bars spaced at 4 in. for 8'-3"
confinement steel
supplementary bottom flange-to-web steel (L-bars)
R-bar

## Slide 78: Test Region B5N
Shear Force
Distance from Beam End
#5 R-bars spaced at 4 in. for 8'-3"
6 in. for 5'-1"
#6 L-bars spaced at 4 in. for 8'-3"
= 1.11
[1.00]
[1.11]
B5N
flexure-shear
6 in. spacing, no L-bars

## Slide 79: Recommended New Design
#4 R-bars (stirrups)
2-#5 L-bars (supplementary steel)
#4 C-bars (confinement)
standard cross-section
Space R-, C-, and L-bars at 4" for 8'-0" (current standard is R-bars at 4" for 6'-0")

## Slide 80: Recommended New Design
3'-0" to 3'-6"
2'-6" to 3'-0"
2'-0" to 2'-6" for beams with skew > 30°
1'-6" to 2'-0" for beams with skew < 30°
CURRENT STANDARD
RECOMMENDED STANDARD

## Slide 81: Recommended New Design
CUT
End-region bottom flange-to-web interface reinforcement, = 1%
Square end block length: 2'-6" to 3'-0"
Square end block length: 1'-6" to 2'-0"
EXISTING TEXAS U-BEAM STANDARD
RECOMMENDED NEW TEXAS U-BEAM STANDARD
R-bar
R-bar
L-bars
End-region bottom flange-to-web interface reinforcement, = 4%
End block vertical reinforcement (V- and F-bars)

## Slide 82: Final Shear Tests
Phase II Beams
Beams 6 and 7 fabricated using recommended new standard design
Beam 6 was square
Beam 7 was skewed 45°
Beam 6
Beam 7

## Slide 83: Test Region B6S
Shear Force
Distance from Beam End
[1.27]
[1.09]
B6S
#4 R-bars spaced at 4 in. for 8'-3"
6 in. for 5'-1"
2-#5 L-bars spaced at 4 in. for 8'-3"
flexure-shear
= 1.27
6 in. spacing, no L-bars

## Slide 84: Test Region B7N
B7N
web crushing
= 1.65
Shear Force
Distance from Beam End
[1.33]
[1.65]
#4 R-bars spaced at 4 in. for 8'-3"
6 in. for 5'-1"
2-#5 L-bars spaced at 4 in. for 8'-3"
6 in. spacing, no L-bars

## Slide 85: Effect of Design Changes
[0.56]
[0.72]
Shear Force
Distance from Beam End
= 0.56
B2N
Horizontal Shear Failure
Shear Force
Distance from Beam End
[1.27]
[1.09]
= 1.27
Flexure-Shear Failure
B6S

## Slide 86: Comparison to the Literature
Concrete Strength [ksi]
calculated using AASHTO LRFD General Procedure (2010)
conservative

## Slide 87: Comparison to the Literature
Concrete Strength [ksi]
calculated using AASHTO LRFD General Procedure (2010)
conservative
B5N
B6S
B7N

## Slide 88: SHEAR STRENGTH: Horizontal Shear in Prestressed Beams

## Slide 89: Horizontal Shear in Prestressed Beams
P
Find horizontal stress on interface and use it to calculate demand
Calculate capacity following shear-friction theory, giving credit to cohesion between concrete sections and clamping force from reinforcement
To verify method, compared demand to capacity at a single point for laboratory tests

## Slide 90: Calculation Method
Horizontal Shear Demand:
average horizontal shear stress
distance from centerline of bearing pad to the ultimate evaluation point
UEP
45°

## Slide 91: Calculation Method
Definition of average horizontal shear stress:
Complementary property of shear
Non-linear analyses showed that average stress was a reasonable approximation of the stress at the critical interface

## Slide 92: Calculation Method
Horizontal Shear Capacity:
steel friction / clamping term
concrete cohesion term
prestress transfer penalty
beam shape / reinforcement detailing factor

## Slide 93: Calculation Method
Horizontal Shear Capacity:
AASHTO shear friction equation

## Slide 94: Calculation Method
Horizontal Shear Capacity:
prestress transfer penalty
Bars near beam end are stressed at prestress transfer, to resist a force equal to 4% of

## Slide 95: Calculation Method
Horizontal Shear Capacity:
beam shape / reinforcement detailing factor

## Slide 96: Horizontal Shear Evaluation Database
Subset of UTPCSDB Evaluation-Level I Database
Specimens removed if:
  post-tensioned
  rectangular or T-shaped
  non-standard beam section
  skewed beam
  insufficient reinforcement information available
HSED contains 69 data points (including 8 U-Beams)

## Slide 97: Horizontal Shear Evaluation Database
Texas 4B28
AASHTO Type I
AASHTO Type II
Texas Type C
AASHTO Type II with deck
AASHTO Type III with deck
Minnesota Type 54
Texas Tx70 with deck
PCI BT-63 with deck
Texas Tx46 with deck
PCEF-45
Texas Tx28 with deck
Minnesota Type 54 with deck
Texas 5B40
Texas 5XB40 with deck
Texas U54 with deck
Texas Modified U54 with deck

## Slide 98: Horizontal Shear Evaluation
1.0
exceed calculated shear capacity
1.0
horizontal shear damage expected
[calculated using AASHTO General Procedure]

## Slide 99: Horizontal Shear Evaluation
1.0
exceed calculated shear capacity
1.0
horizontal shear damage expected
U-Beams
[ Phase I ]
most beam tests
U-Beams
[ Phase II ]
[calculated using AASHTO General Procedure]

## Slide 100: Horizontal Shear Evaluation
NO horizontal shear damage
[calculated using AASHTO General Procedure]

## Slide 101: Horizontal Shear Evaluation
SOME horizontal shear damage
[calculated using AASHTO General Procedure]

## Slide 102: Horizontal Shear Evaluation
Some Horizontal Shear Damage
No Horizontal Shear Damage
[calculated using AASHTO General Procedure]

## Slide 103: Horizontal Shear in U-Beams
Some Horizontal Shear Damage
No Horizontal Shear Damage
[calculated using AASHTO General Procedure]

## Slide 104: Horizontal Shear in U-Beams
including
without
Some Horizontal Shear Damage
No Horizontal Shear Damage
[calculated using AASHTO General Procedure]

## Slide 105: Horizontal Shear in U-Beams
What is and where did it come from?

## Slide 106: HSED without U-Beams
Some Horizontal Shear Damage
No Horizontal Shear Damage
[calculated using AASHTO General Procedure]

## Slide 107: HSED with U-Beams
Some Horizontal Shear Damage
No Horizontal Shear Damage
[calculated using AASHTO General Procedure]

## Slide 108: Horizontal Shear in U-Beams
#1
#1
#2
#2

## Slide 109: Horizontal Shear in U-Beams
#1
#1
#2

## Slide 110: Shear Friction
Reinforcement

## Slide 111: Shear Friction
Side view of theoretical shear friction specimen with distributed reinforcement
Side view of theoretical shear friction specimen with asymmetrical reinforcement

## Slide 112: Horizontal Shear in U-Beams
P
P
critical plane

## Slide 113: Horizontal Shear in U-Beams
WEB
Bottom Flange
12 in.
5 in.
Critical Interface

## Slide 114: Horizontal Shear in U-Beams
WEB
Bottom Flange

## Slide 115: Horizontal Shear in U-Beams
P
P
2.25in.
CENTERED BAR SPECIMEN
1in.
OFFSET BAR SPECIMEN

## Slide 116: Horizontal Shear in U-Beams
critical interface
bottom flange
web

## Slide 117: Horizontal Shear in U-Beams
bottom flange
web

## Slide 118: Horizontal Shear in U-Beams

## Slide 119: Modified Push-Off Results
Calculated capacity = 74.4 kip
 |  | Centered | Offset
Series 1 | Measured Value | 67.4 kip | 54.7 kip
Series 2 | Measured Value | 73.2 kip | 60.1 kip

## Slide 120: Modified Push-Off Results
Calculated capacity = 74.4 kip
 |  | Centered | Offset
Series 1 | Measured Value | 67.4 kip | 54.7 kip
 | Ratio to Calculated | 0.91 | 0.73
Series 2 | Measured Value | 73.2 kip | 60.1 kip
 | Ratio to Calculated | 0.98 | 0.81

## Slide 121: Modified Push-Off Results
 |  | Centered | Offset | Ratio: | Offset | 
 |  |  |  |  | Centered | 
Series 1 | Measured Value | 67.4 kip | 54.7 kip | 0.81 |  | 
 | Ratio to Calculated | 0.91 | 0.73 |  |  | 
Series 2 | Measured Value | 73.2 kip | 60.1 kip | 0.82 |  | 
 | Ratio to Calculated | 0.98 | 0.81 |  |  | 
for U-Beams with offset reinforcement (i.e., no supplementary bars), reduce capacity with equal to 0.8

## Slide 122: Horizontal Shear Evaluation
Some Horizontal Shear Damage
No Horizontal Shear Damage
[calculated using AASHTO General Procedure]

## Slide 123: My Contributions to the Literature
Shear Test Program
Box-Beam 23 (2%)
T-Beam 139 (12%)
Rectangular 299 (26%)
I-Beam 677 (59%)
U-Beam 11 (1%)
[ data from UTPCSDB Filtered Database, N = 1138 ]

## Slide 124: My Contributions to the Literature
Shear Test Program
[ data from UTPCSDB Filtered Database, N = 1138 ]
Specimen Depth [in.]
Year of Testing
50%
2%

## Slide 125: My Contributions to the Literature
Shear Test Program
Specimen Depth [in.]
Year of Testing
U-Beams: 62.75 in.
[ data from UTPCSDB Filtered Database, N = 1138 ]
50%
2%

## Slide 126: My Contributions to the Literature
Shear Test Program
Shear Area, [in.2]
Year of Testing
60%
1%
[ data from UTPCSDB Filtered Database, N = 1138 ]

## Slide 127: My Contributions to the Literature
Shear Test Program
Shear Area, [in.2]
Year of Testing
U-Beams:
550 to 940 in.2
[ data from UTPCSDB Filtered Database, N = 1138 ]
60%
1%

## Slide 128: My Contributions to the Literature
Horizontal Shear Evaluation Method
  Used existing theories and equations to present a method for calculating the likelihood of a horizontal shear failure in a prestressed concrete beam
  Determined an appropriate factor to account for asymmetry present in U-Beam reinforcement design
  Verified the method using data from the literature

## Slide 129: My Contributions to the Literature
Fixed a problem in a Texas beam standard
Beams built following recommended new design
Failed in typical web-shear modes up to 65% above the calculated vertical shear capacity
Beams built following existing details
Failed in an unusual mode at shears up to 44% below the calculated vertical shear capacity

## Slide 130: Questions or Comments?

## Slide 131: Crack Widths
Applied Shear / Measured Capacity
Maximum Measured Crack Width [in.]

## Slide 132: Temperatures
Skewed End of Beam 1
A
Skewed End of Beam 2
B
70
95
120
145
170

## Slide 133: Conclusions from Shear Study
Loads applied over the webs distribute
to the two webs evenly in square beams
The shorter web of the square/skew beams took more load at the skewed end

## Slide 134: Load Distribution
Strong Floor
Load in load cells used to estimate load in webs
Steel Load Transfer Plate
Load Cell
Elastomeric Bearing Pad

## Slide 135: Load Distribution
Strong Floor
Load in load cells used to estimate load in webs
Distribution of Load:
EAST
Load Cell
[ ]
WEST
Load Cell
[ ]

## Slide 136: Load Distribution
West Load Cell / Total End Load
Applied Shear / Failure Shear
B5N
SW
SE
Test Region
West Load Cell / Total End Load
Applied Shear / Failure Shear
B1S
Test Region
SW
SE

## Slide 137: Load Distribution
West Load Cell / Total End Load
Applied Shear / Failure Shear
B1S
Test Region
SW
SE
West Load Cell / Total End Load
Applied Shear / Failure Shear
B7N
SW
SE

## Slide 138: Conclusions from Shear Study
Performing calculations as if the two webs act as one unit is a reasonable and conservative assumption

## Slide 139: Conclusions from Shear Study
When the strength of the bottom flange-to-web interface is such that typical web-shear failure modes control, observed strength consistently exceeded calculated values
Compare to the UTPCSDB-2011 Evaluation Database (Level II)…

## Slide 141: Flow of Test Program

## Slide 142: Test Region B6S
area with R- and L-bars spaced at 4 in.
area with R-bars spaced at 6 in.

## Slide 143: Test Region B7N
area with R- and L-bars spaced at 4 in.
area with R-bars spaced at 6 in.

## Slide 144: Horizontal Shear in Prestressed Beams
PCI BT-63
from Hawkins & Kuchma (NCHRP)
Tx46
tested at FSEL 06/2010

## Slide 145: Horizontal Shear in Prestressed Beams
Texas U54